## Slide 1: DRIVING SUPPLY CHAIN RESILIENCE AND REGIONAL DEVELOPMENT THROUGH INDUSTRIAL 3D MANUFACTURING
Presenters:
Dr. Gabriel Farotade- Senior Deputy Manager, Advanced Manufacturing
Adedoyin Yusuf- Manager, Business Development
W E S T A F R I C A I N D U S T R I A L I Z A T I O N , M A N U F A C T U R I N G & T R A D E S U M M I T 2 0 2 6

## Slide 2: Presentation Roadmap
01
02
The West African Landscape
Supply Chain Pain Points in West Africa
03
Smart Manufacturing - Industrial 3D Manufacturing
04
Circular Economy: Bridging the Gap via Local Manufacturing
05
Quality Framework: Process & Part Qualification
06
Case Studies: One Layer at a
Time
01
The West African Landscape: Current State, Challenges and Opportunities
02
Supply Chain Pain Point Analysis:
Supply chain fragility, import dependency, downtime costs
03
Smart Manufacturing – Strategic Economic Enabler: Non-metallic (SLS, FFF, LFAM) & Metallic (CSAM, SLM, WAAM)
04
Circular Economy: Harnessing West Africa’s Natural Resources to create new regional markets
05
Quality Framework: Process qualification (API 20S, ISO 17296), part
certification
06
Case Studies: Components manufactured by RusselSmith using Industrial 3D manufacturing for the oil & Gas Sector in Nigeria.

## Slide 3: The West African Landscape
477 million
Total Population
5.5 million (1.16%)
Annual Population Growth
$693 billion
Total Combined GDP (2025)
World Population Review, 2026
PwC: 2026 West Africa Economic Outlook
IIAG Data Portal: Economic Community of West African States (ECOWAS)
West African Health Organisation
ABANEME, A.O., MGBACHI, P.U. and Chioma, E., 2024. Challenges of Economic Community of West African States (ECOWAS) on promotion of democracy and good governance in West African Sub-region. Alvan Journal of Social Sciences,(AJSS), 1(1), pp.1-16.
4.3%
GDP Growth Rate (2025)
Key Economic Drivers
New oil and gas production from Senegal and Niger
Rising Oil & Gas outputs
Continued domestic demand
Expanding infrastructure and energy projects
Challenges
Poor infrastructure (power, transportation)
Regulatory misalignment hindering trade (Trade Barriers)
High dependence on raw materials export
Weak development finance institution
Opportunities
Development of the AfCFTA and ECOWAS Trade Liberalization Scheme
Rising volume of local manufacturers
Increasing global demand for critical minerals vs WA’s mineral wealth

## Slide 4: Supply Chain Pain Points in West Africa
Import Dependency & Forex Exposure
High percentage of industrial parts imported from EU, Asia, North America
Currency devaluation adds 25–40% cost volatility year-on-year
Single-source OEM lock-In: no alternative suppliers in-region
Port congestion (Lagos, Tema): avg 21- day clearance delays
Lead Time & Downtime Crisis
Critical spare lead time: 8–16 weeks
Unplanned downtime cost: $150K–
$500K/day (upstream O&G)
Safety stock requirement: 6–12 months inventory holding
Obsolescence risk: discontinued parts force entire system redesign
Manufacturing Capability Gap
Limited precision machining: ±0.5mm tolerance ceiling regionally
Lack of high-temp alloy casting facilities (Inconel, Ti-6Al-4V)
Welding/fabrication only — no advanced joining (e.g., HIP, diffusion bonding)
Limited local production capacity for legacy or discontinued components
Quality & Certification Bottleneck
No regional NDT labs for RT/UT/CT with API/ASME accreditation
Material traceability non-existent: untraceable supply chains
Third-party inspection requires fly-in experts: $50K–$100K/event
Process qualification infrastructure absent (heat treat, HIP, shot peen)
Skills & Knowledge Deficit
Workforce trained in traditional/subtractive technology only
No regional metrology capability (CMM, CT scanning, GD&T)
R&D fragmentation: universities disconnected from industry needs
Brain Drain: trained engineers emigrate due to lack of local opportunity
Extensive Inventory Costs
Increased inventory carrying costs due to hold large safety stock levels
Overstock of critical components to avoid operational shutdowns
Oversized local inventories due to lack of responsive regional manufacturing capacity
Bulk purchasing, increasing warehousing, and obsolescence costs

## Slide 5: Opportunity Gaps
What is the untapped opportunity?
High recurring demand for
MRO spare parts
Predictable failure patterns
of legacy equipment
Large import substitution potential
AfCFTA enabling regional trade integration
Growing offshore oil, marine, defence, and other sectorial needs

## Slide 6: Smart Manufacturing: Industrial 3D Manufacturing
uses heat to cause atom diffusion across particle boundaries, fusing them together without turning the material into a liquid
Melting in additive manufacturing (AM) is a phase transition process where a solid material (powder or wire) is heated, often via laser or electron beam, to its liquid state to create 3D objects
Melting
a premier vat photopolymerization 3D printing technology that uses a UV laser to selectively cure liquid resin into hardened plastic, layer-by-layer.
Stereolithography
What is Industrial 3D Manufacturing?
“a computer-controlled process that creates physical, three-dimensional objects by depositing materials, such as plastics, metals, or ceramics, layer-by-layer based on a digital 3D model.”
Types of 3D Manufacturing Processes
Sintering

## Slide 7: Smart Manufacturing: Industrial 3D Manufacturing
Fused Filament Fabrication (Material Extrusion)
Fused Granule Fabrication (Material Extrusion)
Wire Arc Additive Manufacturing (Direct Energy Deposition)
Selective Laser Melting (Powder Bed Fusion)
Cold Spray Additive Manufacturing (Solid State
Additive Manufacturing)

## Slide 8: Industrial 3D Manufacturing - Materials
Non-Metallic Materials |  | 
Materials | Specific Materials | Applications
Standard |  | 
PLA | Polylactic Acid | Non-functional prototypes; Tooling jigs (low-stress); Cable management clips (non-critical); Interior design mock-ups
ABS | Acrylonitrile Butadiene Styrene | Air vent grilles; Overhead bin components; Seat back components (non-structural); Storage containers; Control panel bezels
PETG | Polyethylene Terephthalate Glycol | Chemical-resistant containers; Transparent gauge guards; Transparent cockpit components (prototypes); Protective shields (equipment)
Nylon (PA) | Polyamide (PA6 / PA12) | Wear-resistant bushings (low-load)• Tool holders & clips• Valve handle grips; Ducting & air management• Interior brackets
TPU | Thermoplastic Polyurethane | Protective hose sleeves; Gaskets & seals (low-pressure); Flexible cable protection; Anti-slip surfaces; Flexible ducting connectors
ASA | Acrylonitrile Styrene Acrylate | Outdoor equipment housings; UV-resistant enclosures; Exterior antenna housings; UV-resistant panels
PP | Polypropylene | Chemical-resistant containers; Flexible hinge components; Flexible hinge applications; Corrosion-resistant brackets
High-Performance |  | 
PEEK | Polyether-ether-ketone | Performs reliably in HP/HT downhole environments and subsea valve seats, cable insulation, and bearing components. Meets NACE MR0175 suitability criteria.
PEKK | Polyether-ketone-ketone | Suited for structural subsea brackets, chemical injection manifold components, and ROV tooling
PPSU | Polyphenylsulfone | Preferred for components exposed to steam cleaning cycles, high-pressure water injection, and produced water streams. Used in valve bodies and fluid handling parts
ULTEM (PEI) | Polyetherimide | Used in topside electrical enclosures, junction boxes, and cable management systems in Zone 1/2 hazardous areas
PVDF | Polyvinylidene fluoride | Widely used for chemical injection tubing, pipe liners, and valve seats in sour service (H2S) and chlorinated water systems

## Slide 9: Industrial 3D Manufacturing - Materials
Metallic Materials |  | 
Materials | Specific Materials | Applications
SS316L | Stainless Steel 316L | Valve bodies (HP/HT service); Subsea manifold parts; Pump impellers & casings; Pipeline flanges & fittings, Engine mount brackets; APU components; Landing gear parts; Vehicle suspension brackets; Weapon mount interfaces; Missile body sections
Al-6061 | Aluminium Alloy 6061 | Offshore platform walkways; Cable trays & supports; Non-pressure piping supports; Lightweight tool fixtures; Seat structures; Interior brackets & mounts; Lightweight deck fittings; UAV/drone airframes; Portable equipment housings; Vehicle body panels
AlSi10Mg | Aluminium-Silicon-Magnesium | Heat dissipation housings; Topside equipment brackets; Air intake manifolds; Heat exchangers; Avionics housings; Handheld device chassis
Ti-Gr5 | Titanium Ti-6Al-4V | HP/HT valve components (sour gas); Subsea connector components; Drilling tool components; Turbine blades (gas compression); Turbine blades & discs; Engine casings; Compressor components; Landing gear parts
Cu | Pure Copper (C101/C110) | Thermal management plates; Induction heating coils; RF waveguides (offshore comms); Propulsion motor windings; Sonar transducer housings; Directed energy weapon heat sinks
Nickel Aluminium Bronze | NAB (C95800 equiv.) | Subsea pump impellers• Valve stems & seats (seawater service); Amphibious aircraft parts; Corrosion-resistant fasteners; Torpedo casings; Underwater vehicle propulsion
17-4 PH Steel | 17 Ni-4Cr Precipitation Hardened Steel | Torpedo casings; Underwater vehicle propulsion; Actuator housings; Engine mount hardware; Rudder stocks; High-strength fasteners; Small arms barrels & receivers; Weapon trigger mechanisms
Inconel | Inconel 625, 718 | Exhaust systems; Chemical injection systems; Flare tips; Turbine engine components; Combustion chambers; Jet engine hot sections; Missile propulsion components
18Ni300 | Maraging Steel | Drilling bit bodies; Downhole tool housings; Submarine pressure hull penetrations; Gun barrels; Missile casings; Armor-piercing projectiles
CoCr | Cobalt-Chrome Alloys | Pump wear rings; Erosion-resistant nozzles; Pump bushings & seals• Propeller shaft bearings;
HEAs | High Entropy Alloys | Extreme environment valve internals; Erosion/corrosion-resistant coatings; Space-based defense systems

## Slide 10: Industrial 3D Manufacturing Suitability Matrix
Industry Vertical | Best AM Process | Typical Use Case | Lead Time Reduction
Oil & Gas | WAAM, SLM | Valve components, flanges | 75-85%
Maritime | CSAM, FFF, LFAM | Propeller repairs, brackets | 60-80%
Mining | CSAM, WAAM | Wear plates, chutes | 70-90%
Defence/Military | CSAM, LFAM, SLM | Small arms components, Vehicle suspension brackets | 75-90%
Healthcare | SLS, SLA, SLM | Prosthetics and orthotics, clinical wares | 50-70%
Aviation | SLM, WAAM, FFF | Landing gear parts, Cabin air system fittings | 30-65%

## Slide 11: Circular Economy: Bridging the Gap via Local Manufacturing
Non-Metallic Circular Economy: Filament Recycling & Local Material R&D
FFF/LFAM Recycling Loop
1
Scrap Collection Support structures, failed prints, purge waste
2
Sorting & Cleaning
Material segregation,
contaminant removal
3
Shredding & Pelletizing
Granulation to 3–5mm pellets
4
Extrusion into Filament
1.75mm / 2.85mm
diameter control ±0.05mm
5
Quality Testing
Tensile, DSC, MFI, diameter verification
Local Material Development: University & Industry Collaboration
University Partnerships
Polymer chemistry R&D: bio-based filaments from cassava starch, palm oil derivatives Composite development: natural fiber-reinforced polymers (jute, sisal, kenaf)
Thermal characterization labs: DSC, TGA, rheology for process optimization
Joint IP development: locally-optimized materials for tropical climate (high humidity, UV)
Research Institute Collaborations
FIIRO (Nigeria), CSIR (Ghana): food-safe polymers, agricultural waste valorization Material property databases: mechanical testing (ISO 527, 178) for certification Flame retardancy & electrical properties for marine/offshore applications Standards harmonization: align local materials with ISO 17296, ASTM F2792
Target Materials (5-Year Horizon)
High-temp engineering polymers: locally-sourced PEEK alternatives, PSU, PEI Marine-grade composites: corrosion-resistant, UV-stable for offshore structures Recycled content certification: 30–50% post-consumer content with virgin properties Biocomposites: sustainable, low-cost materials for non-critical applications

## Slide 12: Circular Economy: Bridging the Gap via Local Manufacturing
Atomization: The Enabler for Metallic Advanced Manufacturing (AM) Circular Economy in West Africa…
Atomization
AM Scrap Build
Failed Parts from Service
West African Minerals via Mining
AM Certified Powder
Why Atomization is Critical for West
Africa
1. Feedstock Independence
Current: 100% imported metal powder from EU/NA at $80–$250/kg. Atomization: Leverage West African mineral resources (bauxite, iron ore, copper) and AM scrap to produce powder locally at 40– 60% cost reduction.
2. Scrap Valorization
AM generates 5–15% build scrap (supports, failed parts, spatter). Without atomization, this is land-fill waste. Gas atomization (argon/nitrogen) recovers and reprocesses scrap into certified powder (15– 45μm PSD), closing the loop.
3. Quality Control & Traceability
Inert gas atomization (VIGA, EIGA, PREP) produces spherical, low-oxygen powder meeting API 20S feedstock requirements. Regional atomization facilities enable batch traceability, chemistry verification (ICP-MS), and flowability testing per ISO 13320.
4. Strategic Mineral Utilisation
West Africa holds significant reserves of bauxite (Guinea: 7.4B tonnes), iron ore (Liberia, Sierra Leone), and copper (Zambia pipeline). Atomization infrastructure converts raw/refined metals through beneficiation process and mineral processing into high-value AM feedstock, moving up the value chain from commodity export to advanced manufacturing input.
Why Atomization is Critical for West Africa

## Slide 13: Quality Framework: Process & Part Qualification
PROCESS QUALIFICATION
Feedstock Qualification
Powder: PSD (ISO 13320), flowability (Hall, Carney), chemistry (ICP-MS), O₂/N₂ content, morphology
(SEM)
Filament: diameter tolerance, tensile (ISO 527), DSC/TGA, moisture content, MFI
Machine Qualification (IQ/OQ/PQ)
Installation Qualification: environmental controls, power stability, inert gas purity
Operational Qualification: build plate flatness, laser/arc calibration, layer thickness verification Performance Qualification: witness coupons, mechanical testing per spec, repeatability studies
Process Parameter Development
Design of Experiments (DOE): laser power, scan speed, hatch spacing, layer thickness Thermal profiles: preheat, interlayer dwell, cooling rates (SLM: <10°C/s monitored)
In-situ monitoring: melt pool imaging, thermal cameras, acoustic emission (defect detection)
Operator Certification
AWS D20.1 certification for WAAM operators
ISO 17024 personnel certification for AM technicians
API 20S and 20T training: AMSL classification, traceability, documentation requirements
PART CERTIFICATION & NDT
Non-Destructive Testing (NDT)
Computed Tomography (CT): porosity mapping, internal defects, ±0.05mm dimensional Ultrasonic Testing (UT): volumetric inspection, phased array for complex geometries Radiographic Testing (RT): weld quality, density variation (ASTM E1742)
Magnetic Particle (MT) / Penetrant Testing (PT): surface crack detection
Destructive Testing
Tensile testing: ISO 6892, ASTM E8 (yield, UTS, elongation) Impact: Charpy V-notch (ISO 148), fracture toughness (ASTM E399) Fatigue: HCF/LCF per ASTM E466, Paris Law crack growth
Metallography: grain size (ASTM E112), porosity (ASTM E2109), microhardness (Vickers HV)
Certification & Traceability
Material certificates: Mill certs, powder lot traceability, chemistry verification Build logs: process parameters, environmental data (O₂, humidity), operator ID
Inspection reports: NDT results, dimensional (CMM, GD&T per ASME Y14.5), surface finish (Ra) Third-party certification: API (20S & 20T), DNV, Lloyds Register, ABS (marine/offshore)
Post-Processing Qualification
Heat treatment: stress relief (PWHT), solution + aging, HIP (99.9% density target)
Machining: tolerances, surface finish (Ra ≤ 3.2μm for sealing surfaces)
Coating: HVOF, cold spray, anodizing — adhesion testing per ASTM D4541

## Slide 14: Methodology for evaluating AM feasibility –
Challenge:
Coupling Assembly Connected to the Fire Water Pump on an FPSO damaged due to corrosion
Solution: 3D Manufactured Motor Coupling Hub Replacement
Key decision factor: material replacement from low-carbon steel to high- performance, corrosion-resistant, polymer composite (Carbon PA Pro)
RusselSmith Case Studies: Material/Part Replacement
3D Manufactured Motor Coupling Hub Replacement (Shell, SNEPCo)

## Slide 15: Methodology for evaluating AM feasibility –
INNOVATING FOR RESILIENCE, POWERING PROGRESS
Challenge:
UPVC filter bag housing suffered leakage during operation, resulting in unplanned downtime and disruptions to the freshwater supply
Solution: 3D-manufactured filter housing delivered in 14 days from design approval, compared to conventional manufacturing and international sourcing timelines of 12-15 weeks.
Key decision factor: design optimization potential; from a 3-part assembly to 2 compact units.
ULTEM 9085 material choice due to superior corrosion resistance, strength-to-weight ratio, and long-term durability in offshore and seawater environments.
3D model of the redesigned housing
RusselSmith Case Studies: Design Optimization
From Leaks To Reliability: 3D Manufacturing Of A Replacement Bag Filter Housing For Offshore Desalination (TotalEnergies)

## Slide 16: Methodology for evaluating AM feasibility –
Challenge:
compressor system failure when a rotating component damaged the coupling beyond serviceability.
OEM replacement on a 6-9 months lead time
Solution: Submerged-Arc Additive Manufacturing technique (SAAM) to print the replacement coupling using EM12K wire and BA-S2Si, delivered within 5 weeks
Key decision factors: process technique and material combination suitable for the
dimensional and performance requirements of the component
RusselSmith Case Studies: Significant Lead Time Reduction
3D Manufacturing of Compressor Coupling (Seplat)

## Slide 17: Methodology for evaluating AM feasibility –
Manufacture Time: 40 mins
RusselSmith Case Studies: Agile Production
3D Manufacturing of Solenoid Valve for Defence Military Applications

## Slide 18: From Technology to Strategy- The Value Proposition
Note: Dr. Farotade concludes. Adedoyin takes over here.

## Slide 19: Value Proposition: Supply Chain Sovereignty
Local Manufacturing = Strategic Independence
Rapid Response
On-demand production eliminates long procurement cycles. Parts produced in days, not months.
100%
West African production capability (Nigeria hub, regional expansion)
Traditional Supply Chain
✗ Long international procurement cycles
✗ Shipping delays and customs clearance
✗ Currency exchange risks
✗ Supply chain vulnerability
✗ Limited design iteration
RusselSmith 3D Manufacturing Solution
Rapid local production capability
Responsive consultations and support
Local currency transactions
Secure, controlled environment
Agile design modifications
Cost Efficiency
Reduce inventory costs, eliminate minimum order quantities, and pay only for what you need.

## Slide 20: Industrial 3D Manufacturing as a Strategic Economic Enabler
Industrial 3D Manufacturing is not just a technology but an economic transformation strategy…
On-demand production of Spare Parts
Reducing import dependence in West Africa will enable timely MRO of critical components while strengthening regional value retention and enhancing economic capital within the region.
Lower inventory holding costs
Inventory and warehousing costs can be significantly reduced, as the need for bulk purchasing and maintaining high levels of long-term stock can be effectively eliminated.
Reduced lead times
(Months to Days)
Parts are manufactured and delivered to customers within days, while rapid prototype iterations enable accelerated product validation and faster deployment into the market.
Digital inventory instead of physical stock
Digital twins of components can be developed and securely stored in cloud- based repositories, transforming the digital file into the core product and enabling distributed manufacturing capabilities
Localized manufacturing hubs
Production can be strategically localized within the region based on proximity, thereby reducing logistics costs, shortening turnaround times, enhancing value addition, and strengthening local manufacturing capacity..
Material Waste
Reduction

## Slide 21: Supply Chain Transformation: Quantified AM Impact on West African Operations
Metric | Conventional (Import-Based) | AM-Enabled (Localised) | Improvement
Lead Time (Critical Spare) | 8–16 weeks (import + customs) | 3–10 days (local AM) | ↓ 85%
Cost (Low-Volume <50 units) | Baseline + 60% (duties, freight, FX) | 15–40% reduction vs. import | ↓ 40%
Inventory Holding | 6–12 months safety stock | Digital inventory (on-demand) | ↓ 75%
Material Waste | 60–90% (subtractive machining) | 5–15% (AM + recycling) | ↓ 80%
Sustainability | 18.5 tonnes CO₂e | Reduced Carbon Footprint (3.2 tonnes CO₂e) | ↓ 82%
Supplier Dependency | Single/dual-source OEM lock-in | Digital file: multi-source capable | ↓ 90%
Geometric Complexity | DfM constrained (machining limits) | Near-unlimited (topology opt.) | ∞
Forex Exposure | 100% import in USD/EUR | 70% local content achievable | ↓ 70%
Regional Self-Sufficiency | 0% — full import dependency | 30–50% (5-year target) | +50%
PARADIGM SHIFT: AM + Atomization + Filament Recycling = West Africa transforms from a passive supply chain endpoint into an active manufacturing node with regional sovereignty.

## Slide 22: Decision Framework- When to Use 3D Manufacturing
Off-the-Shelf Parts
Low complexity parts readily available from local suppliers
Batch Production
AM is more cost-effective for low- volume production needs; eliminates MOQ requirement

## Slide 23: Phased Approach to Strategic 3D Manufacturing Integration
REACTIVE
STRUCTURED
01
Digitization and Digital warehousing of Spares
Convert spare part data into digital records for instant access and risk visibility.
Virtual inventory eliminates long-tail supply chain risk for discontinued components
02
Pre-Qualified
Materials Library
Curated library of 3D manufacturing- approved materials ready for rapid deployment on demand
03
Local Production
for Urgent Components
On-demand local 3D manufacturing pathway for time-critical component replacement
OBJECTIVE:
Reduce lead-time exposure across high-impact part families.

## Slide 24: Scaling Local Manufacturing: The RusselSmith Omnifactory
COMPLETED
PHASE 1
2023
Proof of Concept
Smart Factory
Pioneer Status secured
Technology partnerships
established
Initial production capabilities
OPERATIONAL
PHASE 2
FY2026 ✓
Operational Excellence
Omnifactory
Scale production capacity
Multi-technology integration
Regional supply chain hub
ONGOING
PHASE 3
2027+
Continental Leadership
Omnifactory II (MEGA
OMNIFACTORY)
World-class manufacturing scale
Pan-African distribution
Technology innovation center
Vision: One of the world's largest single-site 3D printing facilities serving the African industrial context

## Slide 25: Continental Expansion Strategy
Leveraging AfCFTA for Regional Growth
Priority Markets in West Africa (2026-2028)
ECOWAS integration, strong oil & gas activity Focus:
Ghana – Oil&Gas, Maritime, Infrastructure & renewables focus
Ivory Coast – Mining & energy integration
Senegal – Agricultural Industrialization
Regional Hubs: Establish satellite facilities in 2-3 strategic locations
Expansion Enablers: AfCFTA tariff benefits | Local partnerships | Technology transfer | Regional financing

## Slide 26: Conclusion
Industrial 3D Manufacturing is not just about printing parts; it's about supply chain resilience. Every technical capability discussed, from SLM tolerance to API 20S certification, exists to solve a supply chain failure mode.
West Africa's path to industrial sovereignty runs through the fusion of advanced manufacturing and intelligent supply chain design.